## Slide 1
Vitor E. L. Paiva, José L. F. Freire, Leonardo D. Rodrigues, Gilmar W. R. Delgadillo, Ronaldo D. Vieira
Mechanical Engineering Department, PUC-Rio
SIMULATION AND MEASUREMENT OF RESIDUAL STRESS IN THE WELDMENT OF AN API 5L X60 PIPE

## Slide 2
To simulate the process of welding of API pipes using finite element method
To measure the residual stress in the weldment using two different techniques
To analyze the residual stress caused by the welding
OBJECTIVES OF THIS WORK

## Slide 3
Stress that exists in components and structures in the absence of forces and temperature gradients
The effects of residual stress in structures can be advantageous or disadvantageous
In fatigue the residual stress is considered part of the mean stress for the life estimation
Residual Stress
In welding the residual stress appears in response to the forced heating and cooling of the weldment, which deforms plastic and in a non-uniform way

## Slide 4
The UOE process is divided in 5 steps:
A - The plate edges are first crimped into circular arcs
B – Conformation of the plate in the “U” shape
C – Conformation of the plate in the “O” shape
UOE Fabrication Process

## Slide 5
D – Initially a small pass of GMAW is done to ensure that the pipe is close, after that a full SAW pass is made to finish closing the pipe
E – Expansion of the pipe is applied in order to improve the circularity
UOE Fabrication Process

## Slide 6
The process of welding can be modeled, for example, as the case were there are three beams with different lengths and the middle beam is heated until it has the same length of the others
The middle beam is individually heated, growing in size until it has the same size of the other two beams
Due to the heating and forced cooling residual stress appears in the system in order to enforce equilibrium and guarantee displacement compatibility
Model for Simulating the Welding

## Slide 7
The thermal-mechanical behavior of the weld joint was simulated using the finite element method and the hypothetical model of the three beams
Finite Element Model
The simulation was divided in two parts:
First part: treated the heat transfer between the weld metal and the rest of the pipe
Second part: treated the mechanical behavior of the joint in function of the thermal deformations

## Slide 8
It was used the software ANSYS, version 14.5
It were used 54916 nodes and 114600 elements
Configurations of the Model
Types of elements used:
    SURF152 – 3D solid element, used for thermal analysis, it has 4 to 10 nodes
    TARGE170 – 3D element, used to represent contacts surfaces
    CONTA174 – 3D element, used to represent contact surfaces, it has 8 nodes
    SOLID186 – 3D solid element with 20 nodes, and 3 degrees of freedom for which node. Used for mechanical analysis

## Slide 9
The specimen was made of an API 5L X60 pipe
The diameter was equal to 323.85 mm (12 ¾”), 9.7 mm of thickness and 200 mm of length
Thermal and Mechanical properties changes with the temperature
Configurations of the Model

## Slide 10
The temperatures in the weld joint can be predicted over the time by a transient heat transfer analysis
Taking into account the three beams hypothesis, the welding initiates with the weld bead being deposited at the fusion temperature of the steel. After that, boundary conditions are applied considering internal and external convective coefficients respectively equals to 15 and 30 W/m²K until all parts of the pipe return to the environmental temperature of 22⁰C
Thermal Part

## Slide 11
Thermal Part
1614,2 Max
1424,6
1235,1
1045,6
856,08
666,56
477,04
287,51
22,0 Min
Distribution of temperatures in the weld after its deposition from 0s to 100s

## Slide 12
The history of temperatures previously obtained was transformed in a thermal load to be imposed into the mechanical model
Stresses and deformations caused by the thermal process were determined by a numerical calculus witch takes into account the elastic-plastic behavior of the material, with the properties changing during the analysis
Mechanical Part

## Slide 13
Mechanical Part
Distribution of Von Mises (Equivalent) Stress in the weldment from 0s to 5000s (thermal equilibrium)

## Slide 14
To measure the residual stress generated in the welding process two techniques were applied
Hole-Drilling technique
Elliptical Hole technique
Were used 15 unidirectional strain gage type EA-06-I25AC-350
Were used 57 tri-directional strain gage rosettes PA-06-062RE-120
Experimental Procedure

## Slide 15
The hole-drilling technique consists of machining a small hole in the component, then measuring the deformation caused by the introduction of the hole
Experimental Procedure

## Slide 16
The elliptical-hole technique consists of machining long cuts in the surface of the component, then measuring the deformation caused by the introduction of the cuts
Experimental Procedure

## Slide 17
Experimental Procedure

## Slide 18
Experimental Procedure
Surface for placing the strain gages
Pipe specimen
Lateral plate used to transmit force to the pipe
Strain gages used to measure the applied force
Instrumented bolts
Nuts for force application
Bearings in contact to the floor
Test bench

## Slide 19
The figure shows the evolution of the temperature in the weldment along the time, after the weld bead has being deposited and cooled using two convection conditions
Results
time
Temperature of a point in the weld bead over time
Temperature

## Slide 20
Initially the weld bead is totally expanded and at fusion temperature
Results
In the proportion that the weld bead is cooled it is forced to return to it’s initial size, being in traction; the rest of the joint being in compression, to equilibrate the sum of the forces in the pipe

## Slide 21
Results

## Slide 22
Results

## Slide 23
Conclusions
The FEM can be used as an accurate method to predict the behavior of the residual stresses
It was possible to predict the values of the longitudinal residual stress in the pipe caused by the welding
High values of residual stress were founded in the weldment, some of than were at the same level of the material’s yield strength

## Slide 24
Thank You

## Slide 25
Next Steps

## Slide 26
Next Steps

## Slide 27
Next Steps